## Slide 1: Raw material
Three groups

## Slide 2
Plastic material- clay
Non-plastic or leading mixtures- silica
Fluxes/ mineralizers- promotes formation of liquid phase- feldspar
Raw material is
clay + feldspar + sand

## Slide 3
Feldspar is present in crystalline rocks (as granite/gneiss)
Granite- unstratified, granular rock
Gneiss – laminated rock (arranged in layers)
both has quartz, feldspar, mica
* Feldspar attacked by atmospheric carbonic acid (CO2 + H2O) and undergo decomposition with formation of alkali carbonate, aluminium silicate and sand

## Slide 4
Aluminum silicate in hydrate form is Kaolinite and main constituent of kaolin/white china clay

## Slide 5: Raw material
Kaolinite | feldspar | Sand/flint
Al2O3.2SiO2.2H2O | K2O.Al2O3.6SiO2 | SiO2
plastic | Non-plastic | Non-plastic
refractory | Easily fusible | refractory
1785oC | 1150oC | 1710oC
Much shrinkage | fuses | No shrinkage

## Slide 6
Clay is important in production of porcelain , stone and earthen ware- since it forms with water a plastic mass which becomes hard and stone like when heated to high temperature
Clays are plastic and mould able when sufficiently finely pulverized and wet, rigid when dry and vitreous when fired at a higher temperature

## Slide 7: Three types or feldspar
Potash feldspar-K2O.Al2O3.6SiO2 (orthoclase/microline)
Soda/albite – Na2O.Al2O3.6SiO2
lime- CaO.Al2O3.6SiO2

## Slide 8: Other ingredients
Used as a fluxing agent(which lower temperature) and special refractory material

## Slide 9: Fluxing agents
Borax Na2B4O710H2O * iron oxides
Boric acid *lithium minerals
Barium materials *antimony oxides
Soda ash fluorspar
Sodium nitrate
Calcined bones
Cryolite
Lead oxides

## Slide 10: Special refractory materials
Alumina *magnesite
Zirconia *carborundum
Titania * aluminium silicate
Thoria
Chromite
Lime
Lime stone
Dolomite
mullite

## Slide 11: manufacture
For both glazed and unglazed
Unglazed manufactured- then apply glaze either before of after firing
Steps

## Slide 12: 1) Grinding of raw materials
* raw materials other than clay are ground finely- mix with clay to get uniform mixture
Done by- weathering, calcination, mechanical crushing machines
Subsequently reduced to fine size by – pan mills, edge roller mills, ball/pebble mills

## Slide 13: 2) Mixing or preparation of bodies
Mixed in definite proportion to have specific property
Mixed with required amount of clay and water in a tank called as blunger
Creamy layer passes through a sieve to separate coarse particles
Pass through an electromagnetic set to remove iron bearing particles

## Slide 14
Mixing done by following methods
Clay is manipulated in a plastic state, either soft or stiff
Clay mixed in dry state and add required water
Dissolve clay in water, mix clay with dry or wet pulverised non-plastic material and remove water in filter press

## Slide 15: 3) Body preparation using clay in plastic state
Since plastic clay is very sticky mixing is not very intimate
Thorough mixing- if plastic materials are dried and then crushed
Mixing of various materials is done in alsing cylinders, dust mills, rotating propeller machines

## Slide 16: 4) Body preparation using clay slip
i) filtering
* mixed mass called slip is pumped into filter presses to remove excess water
Filter press is used for turning the water slip into a plastic body
The solid part of slip- is a plastic body called as filter cake
Rotary vacuum filters can also be used

## Slide 17
ii) Kneading
* filter cake from filters are put into pug mill, which is used to mix the material in plastic or semi plastic state
Vertical or horizontal plug mills are used
Throwing is the process by which different shapes are given to clay mass- like potters wheel

## Slide 18
Articles other than round shape are formed in plaster moulds
For articles of irregular form plaster or plaster of Paris moulds are used- plaster of paris absorbs water from clay and does not adhere the soft clay, so clay can be easily removed from the body.

## Slide 19
iii) Jollying
mechanical process of making a large number of similar articles through moulds economically
iv) Slit casting
*Process of giving shapes to clay wares from clay liquid- used for articles of complex shape, refractory, cheap and reusable moulds, dinner ware, plumbing ware

## Slide 20
V) pressing
process for making plastic, semi-plastic and powder bodies
Plastic- tiles, roofings, drain pipes
Powder- wall/floor tiles

## Slide 21
Vi) extrusion
forcing plastic paste through a die or mouth piece of required shape.
vii) Turning
dune in lathes- before turning a ceramic body, body should be dried to reasonable hard state
Medium /large particles- body can be in semi hard state
Small articles- (spark plug) turned in hard state

## Slide 22: 5) Drying
Articles dried well before firing
Imperfect drying causes craking of articles during firing
Speed of drying depends on
* shape of article
* temperature of surrounding air
* rate of air circulation
* humidity content of surrounding air

## Slide 23
Dried in – intermediate driers(lifts, hot floor), semi continuous dryer(dobbins), continuous dryer( tunnel dryers and mangles)
Nowadays drying by- IR/high frequency

## Slide 24: 6) Firing
Clay materials acquire durability /other qualities when heated at high temperature.
Finally dried articles are known as - blanks
Glaze is put on blanks before firing
In most cases blanks are fired to produce bisques/biscuits- then put glaze on cold biscuits and then fire

## Slide 25
During firing the following happens
dehydration- rate maximum at 500oC
Oxidation- between 300-900oC- sulphur and iron compounds are oxidized
Decomposition- of carbonates of Ca/Mg
Vitrification or melting- to cover up and bond the unmelted mass or particles on cooling- volume reduces – 950-1050oC

## Slide 26
V) reduction- colour dilution of processed articles- cut air supply to kiln
vi) annealing- slow cooling to fired clay
vii) decoration

## Slide 27: 7) Glazing
Important in white/ table wares
Glaze- a thin coating of glass that is melted on to the surface of the more or less porous ceramic material.
Glaze is a fine powder consisting of a mixture of glass forming material of proper composition-like lead silicates, boro silicates

## Slide 28
Glaze contains – feldspar, silica, china clay, soda, potash, fluorspar, borax
Glazing done by- dripping, spraying, pouring, brushing of glaze material on dry blanks of clay material

## Slide 29: Glazing done for
Decorative effect
Improve appearance of article
Improve durability of ceramic material
To provide smooth and glossy surface
To protect article from environmental and atmospheric effects
To make surface impervious to liquids.